## Slide 1
Kenneth Hanson
Department of Chemistry & Biochemistry
Florida State University, Tallahassee, FL, USA
Understanding and Controlling Molecular Excited State Processes Using Metal Oxide Interfaces

## Slide 2
Molecular Photochemistry/Photophysics
Molecule
phosphorescence
fluorescence
internal
conversion
intramolecular charge transfer
electron transfer
proton transfer
energy transfer
excimer formation
exiplex formation
photochemical transformation
hn
conformational change

## Slide 3
Molecular Photochemistry/Photophysics
Sundström et al. J. Phys. Chem. B 1999, 103, 2327-2346.
Lundholm et al. RSC Adv. 2014, 4, 25502-25509.
Energy Transfer
Electron Transfer

## Slide 4: Structural Control: Humans
Kent et. al. J. Am. Chem. Soc., 2010, 132, 12767
Ma et. al. Nature Protocols, 2013, 8, 439
Phospholipid Bilayers
Metal Organic Frameworks
Polypeptides
Slate et. al. J. Am. Chem. Soc., 1998, 120, 4885
Crystals
Zhu et. al. J. Phys. Chem. C, 2014, 118, 14150

## Slide 5: Metal Ion-Linked Multilayer
NanoMO2
Energy/e- Cascade
Control e- Transfer
Singlet Fission
Photon Upconversion
5

## Slide 6
hn → hn
hn → hn
hnex
S1
S2
S0
S3
IC
IC
hnem
Down Conversion vs. Upconversion

## Slide 7
hn
T1
Annihilator
Sensitizer
S1
T1
S1
S0
(1)
(2)
(3)
(4)
(5)
hn
T1
Annihilator
S1
T1
Sensitizer
S1
S0
2 hn → hn
Photon Upconversion

## Slide 8
(4)
(5)
hn
T1
S1
T1
S1
S0
2 hn → hn
Photon Upconversion
Annihilator
Sensitizer

## Slide 9
Sensitizer-Annihilator Interactions
Solution
MOF
Polymer Films
Neat-solvent
JACS 2013, 135, 19056
JACS 2016, 138, 6541
JACS 2007, 129, 12652
Chem. Commun., 2004, 2860
Photochem. Photobiol. Sci. 2014, 13, 48
Microemulsion
J. Phys. Chem. C, 2013, 117, 14493
Heterogeneous

## Slide 10
Solar Cell Efficiency
Standard solar cell ~33%
Max Theoretical Efficiency
Schulze and Schmidt Energy Environ. Sci. 2015, 8, 103-125
1.3 eV bandgap
Pin = 100 mW/cm2 (AM1.5)
Pmax = J x V
Voc
Large BG
High V, Low J
Small BG
Low V, High J
SQ Limit
1.3 ev
hn
hn
hn
hn
Voc

## Slide 11
Solar Cell Efficiency
Standard solar cell ~33%
Max Theoretical Efficiency
Schulze and Schmidt Energy Environ. Sci. 2015, 8, 103-125
1.3 eV bandgap
Solar cell with upconversion > 45%
1.76 eV bandgap
with TTA-UC
Perovskites, OPV, DSSC
Ekins-Daukes and Schmidt,
Appl. Phys. Lett., 2008 93, 063507.

## Slide 12
Harnessing TTA-UC
J. Phys. Chem. Lett. 2013, 4, 2073.
Chem. Commun. 2012, 48, 209.
hn
hn
Transmission
Light absorption and TTA
Upconverted emission
Absorption by a solar cell
(3)
Solar Cell
(4)
S
A*
A
Upconversion Solution/Film
(2)
(1)
Optical Coupling:

## Slide 13
Harnessing TTA-UC
hn
hn
Transmission
Light absorption and TTA
Upconverted emission
Absorption by a solar cell
(3)
Solar Cell
(4)
S
A*
A
Upconversion Solution/Film
(2)
(1)
Optical Coupling:
No isotropic emission
No self-absorption
Increase sensitizer concentration
Electronic Coupling:
Light absorption and TTA
Photocurrent Generation
S
A*
A
Upconversion Solar Cell
(1)
(2)
e-
Need A* at a charge separation interface!
hn

## Slide 14: Metal Ion-Linked Multilayer
NanoMO2
Hill et al. J. Phys. Chem. Lett. 2015, 6, 4510.
S and A in proximity
A-A interactions
On a charge separation interface
Easy DSSC integration

## Slide 15: Metal Ion-Linked Multilayer
NanoMO2

## Slide 16: TTA-UC Emission
lex = 532 nm (1 W/cm2)
Hill et al. J. Phys. Chem. Lett. 2015, 6, 4510.
Φ = 0.0023

## Slide 17: TTA-UC Emission
Hill et al. J. Phys. Chem. Lett. 2015, 6, 4510.
Castellano et al. J. Phys. Chem. Lett. 2012, 3, 299-303.
Strong TTA Limit
Weak TTA Limit
Slope = 1
Slope = 2

## Slide 18: Mechanism
T1
S1
ISC
S0
ET
hn
S1
ZrO2
CB
VB
T1
E
S0
S
Zn
A
e-
T1
S1
ISC
S0
ET
hn
S1
TiO2
CB
VB
T1
S0
S
Zn
A
hn
Upconverted Emission!
Photocurrent?
e-
e-
D/D+
e-

## Slide 19
TTA-UC Photocurrent
J. Phys. Chem. Lett. 2015, 6, 4510.
On ZrO2: Upconverted Emission
On TiO2: Upconverted Photocurrent
λex = 532 nm
TiO2-ML
Co(bpy)32+/3+
MeCN
V
ZrO2-ML
MeCN
Pt counter electrode

## Slide 20
TTA-UC Photocurrent
On TiO2: Upconverted Photocurrent
TiO2-ML
Co(bpy)32+/3+
MeCN
V
Pt counter electrode
Jsc/Voc greater than the sum of its parts.
Jsc= 0.009 mA/cm2
Demonstrated an integrated TTA-UC solar cell.
h = 1.6 x 10-5 %
ACS Energy Lett. 2016, 1, 3-8.

## Slide 21
Side Note: Efficiency
h = 1.6 x 10-5 %

## Slide 22
Increasing UC Photocurrent (JUC)
JPC Lett., 2018, 9, 5810
9 mA/cm2
ACS Energy Lett. 2016, 1, 3-8.

## Slide 23
Increasing UC Photocurrent (JUC)
JPC Lett., 2018, 9, 5810
9 mA/cm2
ACS Energy Lett. 2016, 1, 3-8.
J. Mater. Chem. A, 2017, 5, 11652-11660.
78 mA/cm2

## Slide 24
Increasing UC Photocurrent (JUC)
JPC Lett., 2018, 9, 5810
158 mA/cm2
JACS 2017 , 139, 10988.

## Slide 25
Increasing UC Photocurrent (JUC)
JPC Lett., 2018, 9, 5810
315 mA/cm2
ACS Energy Lett. 2019, 4, 1458.
158 mA/cm2
JACS 2017 , 139, 10988.

## Slide 26
Increasing UC Photocurrent (JUC)
JPC Lett., 2018, 9, 5810
29 mA/cm2
ACS Appl. Energy Mater. 2020, 3, 29.

## Slide 27
Increasing UC Photocurrent (JUC)
JPC Lett., 2018, 9, 5810
12 mA/cm2
JPC C 2020, 43, 23597.
29 mA/cm2
ACS Appl. Energy Mater. 2020, 3, 29.

## Slide 28
Increasing UC Photocurrent (JUC)
JPC Lett., 2018, 9, 5810
3.5 mA/cm2
12 mA/cm2
JPC C 2020, 43, 23597.
JMC C 2022, 10, 4947.
29 mA/cm2
ACS Appl. Energy Mater. 2020, 3, 29.

## Slide 29
Increasing UC Photocurrent (JUC)
JPC Lett., 2018, 9, 5810
ACS AM&I 2021, 13, 32601.
Performance Limitations:

## Slide 30
Energy and Electron Transfer
Upconversion Trilayer
Triplet Sensitizer
Annihilator
e- Acceptor
Singlet Sensitizer
1A
3A*
1A*
1S
3S*
1S*
1F*
1F
kET1
kex(F)
kex(S)
γTTA
kr(F*)
knr(F*)
ket
kBTET
3F*
ket
kBET2
TiO2
Glass
ACS Energy Lett. 2019, 4, 6, 1458
kBET1
kinj(1A*)
kinj(3A*)
kBeT1
kBeT2
kISC
kTET
kr(1A*)
knr(1A*)
knr(3A*)
kr(3S*)
knr(3S*)
kinj(S*)
kmig

## Slide 31
Energy and Electron Transfer
Photosynthesis
Triplet Sensitizer
Annihilator
e- Acceptor
Singlet Sensitizer
1A
3A*
1A*
1S
3S*
1S*
1F*
1F
kET1
3x1011
kex(F)
>1015
kex(S)
>1015
γTTA
1.0x10-15
kr(F*)
5.9x108
knr(F*)
5.8x108
ket
<106
kBTET
~0
3F*
ket
<106
kBET2
4.4x109
TiO2
Glass
ACS Energy Lett. 2019, 4, 6, 1458
kBET1
1.9x107
kinj(1A*)
4.5x1011
kinj(3A*)
1.6x106
kBeT1
9.5x106
kBeT2
5.5x106
kISC >1012
kTET
1.3x104
kr(1A*)
2.5x108
knr(1A*)
2.3x108
knr(3A*)
4.9x103
kr(3S*)
2.5x102
knr(3S*)
1.7x104
kinj(S*)
1.6x106
kmig
Upconversion Trilayer
https://doi.org/10.48550/arXiv.1608.06913

## Slide 32: Metal Ion Linked Multilayer Structure
Energy/Electron Transfer Cascade
ACS AM&I 2016, 8, 28633
Water Oxidation DSPEC
ACS Omega, 2017, 2, 3901.
H2 Generation
Chem. Sci. 2021, 12, 50.
Molecular Rectifiers
Angew. Chemie. 2018, 57, 15390.
ACS Appl. Opt. Mater. 2023, 1, 1156.
Notes: Kato out of Hokkaido University

## Slide 33: Bilayer Structure
What is known:
Not co-deposition
Metal-ion coordination
Directional E/e- transfer
What is not known:
Surface binding angle
Relative orientation
Controllability

## Slide 34: Polarized Attenuated Total Reflectance
ITO coated glass substrate
monolayer
Evanescent wave
John Thomas Bradshaw , A. PhD. Dissertation, University of Arizona, 2005
JACS 2008, 130, 5, 1572
Prof. Scott Saavedra at UofA:
Measure ATE and ATM
Dichroic ratio
Calculate mean tilt angle

## Slide 35: Metal Oxide-Anthracene Structure
S1
ZrO2, Al2O3
CB
VB
E
S0
e-
CB
TiO2
ITO
ITO
30o
TiO2
38o
ZrO2
37o
Al2O3
44o
1.1±0.3nm
2.2±0.5nm
1.2±0.4nm
0.5±0.1 nm
Roughness:
e-
e-
@0 nm roughness, tilt angle = 22o
Rowlen et al. JPC C 1999, 103, 1525.

## Slide 36: Metal Oxide-Anthracene Structure
S1
ZrO2, Al2O3
CB
VB
E
S0
e-
CB
TiO2
ITO
ITO
30o
TiO2
38o
ZrO2
37o
Al2O3
44o
1.1±0.3nm
2.2±0.5nm
1.2±0.4nm
0.5±0.1 nm
Roughness:
e-
e-
@0 nm roughness, tilt angle = 22o
Prof. Wei Yang at FSU:

## Slide 37: Metal Oxide-Anthracene Structure
S1
ZrO2, Al2O3
CB
VB
E
S0
e-
CB
TiO2
ITO
ITO
30o
TiO2
38o
ZrO2
37o
Al2O3
44o
1.1±0.3nm
2.2±0.5nm
1.2±0.4nm
0.5±0.1 nm
Roughness:
ITO
30o
ITO
31o
PO3H2 vs COOH
e-
e-
Similar angle regardless of metal oxide.
Binding group does not impact angle.
Orientation dictated by molecular structure/packing.

## Slide 38: Multilayer Structure
ITO
ITO
Zn
31o
38o
37o
ITO
ITO
33o
Zn
ITO
Zn
38o
40o
Zn

## Slide 39: Multilayer Structure
ITO
ITO
ITO
Zn
Zn
Zn
31o
38o
39o
37o
40o
75o
ITO
ITO
33o
Zn
ITO
Zn
38o
40o
Zn
First multi-chromohore by ATR.
Subsequent metal ion and layer addition has minimal effect on the binding angle.
FRET

## Slide 40: Structure and Energy Transfer
kET = 3×1011 s-1
 100%
ex 475 nm
ex 475 nm
ex 455 nm
ZrO2-F
ZrO2-P
ZrO2-P-Zn-F
F
P
ZrO2
FRET

## Slide 41: Structure and Energy Transfer
F
P
ZrO2
FRET
= fluorescence QY of F
n = refractive index
J = overlap integral
κ2 = orientation factor
r = distance between F and P
>99% >99% >99% >99% >99%
kET = 3×1011 s-1
 100%

## Slide 42: Moving Forward: Controlling Energy Transfer
MO2
CdII CuII FeII LaIII MnII SnIV ZrIV ZnII
JPE 2017, 8, 022004.
PCCP 2018, 20, 20513.
JPC C 2020, 124, 23597.
JPC C 2018, 122, 9835.
Langmuir 2017, 33, 9609.
Zn
38o
41o
ITO
La
36o
50o
ITO
kET = 5.8×1010 s-1
kET = 3.4×1010 s-1
ET
ET

## Slide 43: Moving Forward: Controlling Structure
Molecular Switches
Inhibiting Distortion

## Slide 44: Inhibiting Distortion
J. Phys. Chem. A 2015, 119, 13, 3181–3193
hn
hn
t = 90 ns
F = 0.04%
t = 2800 ns
F = 6.3%
Steric Bulk
Strategic Surface Binding

## Slide 45: Strategic Surface Binding
1
2
3
Constable et al. Dalton Trans. 2009, 6634

## Slide 46: Transient Absorption
In MeOH
On ZrO2 in MeOH
1
2
3
lex = 500 nm
labs = 690 nm
lex = 500 nm

## Slide 47: Decay Kinetics
1
2
3

## Slide 48: Strategic Surface Binding
1
2
3
t = ×5
t = ×7
t = ×20

## Slide 49: Moving Forward: Controlling Structure
Molecular Switches
Inhibiting Distortion
Atomic Layer Deposition

## Slide 50: Controlling Intermolecular Interactions
Beery, D. et al. J. Mater. Chem. C. 2022.
Up-Conversion
Myong, M. S., et al. J. Phys. Chem. C. 2021.
Excimer Emission
Bae, Y. J., et al. J. Am. Chem. Soc. 2018.
Singlet Fission
Atomic Layer Deposition
Emission
Transient Absorption
Knorr et. al. Molecules 2023, 28, 4835.

## Slide 51: Conclusions
TTA-UC Emission
  On ZrO2: Blue to green upconversion
  Quadratic to Linear Behavior
TTA-UC Solar Cell
  Improvements with component selection
  JUC up to 315 mA/cm2
  Structure matters
Determine Structure (polarized ATR)
  1st layer orientation is MOx independent
  2nd layer dependent on metal and binding group
  Reasonable agreement between ATR and Theory (MM)
Efforts to Control Structure are underway

## Slide 52: Other Projects
68% de
86% yield
50:50, R:S BINOL
Boc-D-Proline
ES Proton Transfer Catalysis/Enrichment
Photomechanical Polymers
Using IRT and CCT to Analyze Exams
h
h
H2 Generation Z-Scheme

## Slide 53: Acknowledgements
  Not Pictured Contributors
  Dr. Sean Hill
  Dr. Tristan Dilbeck
  Dr. Yan Zhou
  Dr. Drake Beery
  Cory Ruchlin (McGill)
  Jonathan Wheeler (NCSU)
  Cody Basquill (FSU)
  Ethan Lambert (FSU)
  Dominic Willadsen (REU)
  Collaborators
  Dr. Raaj Winfred
  Dr. Wei Yang
  Dr. Scott Saavedra

## Slide 54: Questions?
@HansonFSU