## Slide 1
Bistability in Molecular Materials: From Spin-State Switching to Controlling Molecular Spin Qubits
Michael Shatruk
Department of Chemistry and Biochemistry
Florida State University, Tallahassee, FL 32306
REU Photochemistry Café
July 11, 2023

## Slide 2
Inorganic Materials in the Shatruk Group
Itinerant Magnetism & Magnetic Refrigeration
Unconventional Spin Textures
Molecular Spin Qubits
Bres
Spin-State Switching & Hybrid 2D Materials

## Slide 3
Motivation for Research
Electricity is a great thing, but…
  - electrical connections unavoidably add weight and mechanical constraints to the device architecture
  - wires corrode, requiring regular maintenance and/or replacement
Light as an alternative:
  - fibers don’t rust
  - the signal is transmitted with the speed of light
  - lower maintenance costs
  - opto-mechanical actuation
  - optical write/read-out

## Slide 4
State of the Art
Extended-structure materials
  - doped semiconductors (Si, GaP, GaAs, etc.)
  - polymers (CD drives)
Molecular materials:
  - much higher storage density
  - light weight
  - high synthetic tunability
  - precise control over the photophysical properties
Alq3

## Slide 5
Splitting of d-Orbitals by Ligand Field
I– < Br– < Cl– < SCN– < NO3– < F– < OH– < H2O < NCS– < py < NH3 < en < NO2– < PPh3 < CN– < CO
Mn+, d
eg
t2g
10Dq
Octahedral symmetry
Spectrochemical series of ligand-field strength:

## Slide 6
eg
t2g
eg
t2g
HS, S = 2
LS, S = 0
I. Spin Crossover (SCO)
Hauser, A. Top. Curr. Chem. 2004, 233, 49-58
Shatruk, M.; Phan, H.; et al. Coord. Chem. Rev. 2015, 289-290, 62-73
Can we leverage the structural and optical changes that accompany SCO to create multifunctional materials?
Dramatic changes in:
- magnetic moment
- M-L bond lengths
- absorption spectrum (color)
Entropy driven transition
Observed for d4, d5, d6, d7 ions
Triggered by changes in temperature, pressure, or photoexcitation

## Slide 7
Example of Fe(II) SCO Complex
SCO with hysteresis (T ~ 7 K)
d(Fe-N)av, Å | 
123 K (LS) | 210 K (HS)
2.002(4) | 2.184(4)
(ClO4–)2
T1/2 = 196 K
T1/2 = 203 K
LS
HS

## Slide 8
190K
195K
200K
202K
204K
205K
210K
LS State Bleaching
[Fe(tpma)(xbim)](ClO4)2
The abrupt change in color due to drastically different optical properties of the HS and LS states
(ClO4–)2

## Slide 9
1A1
LS
3T1
3T2
1T1
1T2
MLCT
5T2
HS
5E
Electronic transitions
of Fe(II) SCO complexes
h
Irradiation into characteristic absorption bands of the LS species results in a light-induced population of the HS state
Light-Induced Excited Spin-State Trapping (LIESST)
At sufficiently low temperature, the HS state will be trapped until it can acquire enough energy to undergo thermally activated relaxation to the LS state
Photomagnetism (LIESST)

## Slide 10
LIESST in [Fe(tpma)(xbim)](ClO4)2
h
Magnetic
Optical
SQUID
(1)
(2)
(3)
(4)
Phan, H.; Chakraborty, P.; Calm, Y.; Chen, M.; Kovnir, K.; Keniley, L. K.; Hoyt, J. M.; Knowles, E. S.; Besnard, C.; Meisel, M.; Hauser, A.; Achim, C.; Shatruk, M. Chem. Eur. J. 2012, 18, 15805
UV-visible spectrum
500 600 700 800  (nm)
(ClO4–)2

## Slide 11
Combining SCO and Conductivity
[FeII(TPMA)(XBIM)]-(TCNQ)1.5(ClO4)·DMF
DMF
Phan, H.; Benjamin, S. M.; Steven, E.; Brooks, J. S.; Shatruk, M. Angew. Chem. 2015, 54, 823-827

## Slide 12
SCO, LIESST, and Conductivity
Conductivity at 300 K ~ 0.2 S/cm
Phan, H.; Benjamin, S. M.; Steven, E.; Brooks, J. S.; Shatruk, M. Angew. Chem. Int. Ed. 2015, 54, 823-827
For reference:
Semiconductors: 10–6 – 101 S/cm
“Bad” metals: 101 – 103 S/cm

## Slide 13
Conductivity Measurements
Before Cooldown
After Cooldown
12 m gold wire
Fe(tpma)(xbim)]ClO4(TCNQ)1.5
Tiny, brittle, and semi-
transparent crystals
Carbon paste, 4-probe measurement

## Slide 14
Nature to the Rescue!
4 mm
20 nm
submicron
Nephila Clavipes
Steven E. et al., Sci. Technol. Adv. Mater. 2011, 12, 055002
21 nm Au is sputtered onto spider silk fibers, rendering them electrically conducting
The silk wires can be flexed but care should be taken not to over-stretch them

## Slide 15
Conductivity Measurements
4 m spider silk wire
Before Cooldown
After Cooldown
Before Cooldown
After Cooldown
Carbon paste, 4-probe measurement
12 m gold wire
Fe(tpma)(xbim)]ClO4(TCNQ)1.5
Tiny, brittle, and semi-
transparent crystals

## Slide 16
Adapted from: Dugay, J.; Aarts, M.; Gimenez-Marques, M.; Kozlova, T.; Zandbergen, H. W.; Coronado, E.; van der Zant, H. S. J. Nano Lett. 2017, 17, 186-193
SCO nanoparticles on graphene
Deposited by contact printing from the surface of an ethyleneglycol droplet)
NP rods: l ~ 25 nm, d ~ 9 nm
II. Ultrathin SCO Films

## Slide 17
Depositing Molecules on Substrates
Source  | Solution | Gas Phase | Solid
Generality | High | Moderate | Low(?)
Scalability | High | Moderate | Moderate
Purity | Low | High | Moderate
Requirements |  |  | 
e-neutrality | n/a |  | o
solubility |  | n/a | n/a
volatility | n/a |  | n/a
thermal stability | o |  | o
surface stability |  |  | o
 = required o = desired

## Slide 18
Gas-Phase Deposition of SCO Films
180 °C
10–8 mbar
162 °C
10–2 mbar
237 °C
10–9 mbar
190 °C
10–5 mbar
140 °C
10–8 mbar
217 °C
10–9 mbar
160 °C
10–9 mbar
100 °C
10–9 mbar
Kumar, K. S.; Ruben, M. Angew. Chem. Int. Ed. 2021, 60, 7502-7521

## Slide 19
Gas-Phase Deposition of SCO Films
180 °C
10–8 mbar
162 °C
10–2 mbar
237 °C
10–9 mbar
190 °C
10–5 mbar
140 °C
10–8 mbar
217 °C
10–9 mbar
160 °C
10–9 mbar
100 °C
10–9 mbar
Kumar, K. S.; Ruben, M. Angew. Chem. Int. Ed. 2021, 60, 7502-7521

## Slide 20
Gas-Phase Deposition of SCO Films
Adapted from: Naggert, H.; Quandt, E.; Tuczek, F.; et al. Dalton Trans. 2011, 40, 6364-6366
[Fe(H2Bpz2)2(L2)] (L2 = bpy, phen)
Substrates: Si, glass, ITO-coated glass, polymer tape
Thickness: 400-500 nm
T1/2 similar to bulk
SCO more gradual
LIESST effect
Methods:
UV-Vis spectroscopy
DFT
Vacuum deposition
(10–2 mbar, 160-190 °C)

## Slide 21
[Fe(qnal)2] on Au(111)
Adapted from: Atrozi, M.; Sessoli, R.; Mannini, M.; et al. J. Mater. Chem. C 2018, 6, 8885
Thickness: 300 nm
T1/2 similar to bulk
SCO more gradual
LIESST effect
Methods:
UV-Vis, XAS
Vacuum deposition
(10–8 mbar, 350 °C)
From XAS

## Slide 22
Molecular Design Challenge
Cooperativity: strong intermolecular interactions
Challenge: increase the volatility while preserving the abrupt spin transition
Volatility: weak intermolecular interactions
Solution: use asymmetric design by separating the cooperative and “volatilizing” functions
Criteria:
- neutral complexes
- easy synthetic modification
- asymmetric ligand structure
- only chelating (clamping) ligands
Miguel Gakiya

## Slide 23
Synthetic Approach
Introduce the asymmetry of interactions to boost volatility
- the cooperativity will be preserved
- the volatility should be much higher
Gakiya-Teruya, M.; Jiang, X.; Le. D.; Rahman, T. S.; Hebard, A. F.; Shatruk, M.; et al. J. Am. Chem. Soc. 2021, 143, 14563-14572
[Fe(tBu2qsal)2]

## Slide 24
Properties of [Fe(tBu2qsal)2]
T1/2 = 117 K / 129 K
TLIESST = 84 K
Crystals grown by vapor transport at >10–5 mbar & 300 °C
Gakiya-Teruya, M.; Jiang, X.; Le. D.; Rahman, T. S.; Hebard, A. F.; Shatruk, M.; et al. J. Am. Chem. Soc. 2021, 143, 14563-14572

## Slide 25
Thin-Film Capacitor
Sublimation
T1/2 ≈ 122 K / 127 K
Gakiya-Teruya, M.; Jiang, X.; Le. D.; Rahman, T. S.; Hebard, A. F.; Shatruk, M.; et al. J. Am. Chem. Soc. 2021, 143, 14563-14572

## Slide 26
Mechanical Exfoliation
van der Waals gaps
Mechanical exfoliation:
Successful exfoliation down to a single molecular layer (1.7 nm thickness)
Koptur-Palenchar, J. J.; Gakiya-Teruya, M.; Shatruk, M.; Zhang, X. X; et al. Under Review

## Slide 27
Mechanical Exfoliation
Mechanical exfoliation:
Successful exfoliation down to a single molecular layer (1.7 nm thickness)
Koptur-Palenchar, J. J.; Gakiya-Teruya, M.; Shatruk, M.; Zhang, X. X; et al. Under Review

## Slide 28
Thickness Dependence of SCO
The normalized reflection contrast measurements suggest increased hysteresis in the 2D SCO material
Bulk
13 L
10 L
5 L
Koptur-Palenchar, J. J.; Gakiya-Teruya, M.; Shatruk, M.; Zhang, X. X; et al. Under Review

## Slide 29
Thickness Dependence of SCO
Hypothesized reason:
Interfacial strain combined with the restriction of domain wall motion
# of layers | T1/2
Bulk | 12 K
13 | ~45 K
10 | ~90 K
5 | ~200 K
Koptur-Palenchar, J. J.; Gakiya-Teruya, M.; Shatruk, M.; Zhang, X. X; et al. Under Review

## Slide 30
2D Heterostructures
Assembled by the PDMS stamp method
Koptur-Palenchar, J. J.; Gakiya-Teruya, M.; Shatruk, M.; Zhang, X. X; et al. Under Review

## Slide 31
2D Heterostructures
Assembled by the PDMS stamp method
Charge transfer blocked by hBN
The Förster energy transfer still allowed
Koptur-Palenchar, J. J.; Gakiya-Teruya, M.; Shatruk, M.; Zhang, X. X; et al. Under Review

## Slide 32
What’s Next?
Investigating heterostructures
Tuning the SCO temperature
d(N–N) in the free, non-coordinated ligand
(experimental or calculated values)
Phan, H.; Hrudka, J. J.; Igimbayeva, D.; Lawson Daku, L. M.; Shatruk, M. JACS 2017, 139, 6437-6447

## Slide 33
Summary
Using the principle of asymmetric design, we can engineer increased volatility of materials while preserving the abrupt SCO
The structural hierarchy allows mechanical exfoliation of ultrathin SCO flakes
Future Efforts
Elucidating the role of substrates
Extending the approach to other types of magnetic molecules (SMMs, radicals)
Investigation of heterostructures and devices with inorganic 2D materials

## Slide 34
The Team
Collaborators
Prof. Stephen Hill and Robert Stewart
(Florida State)
Prof. Arthur Hebard and Juanyuan Xiang;
Prof. Xiao-Xiao Zhang and John Koptur-Palenchar
(University of Florida)
Funding
Prof. Hoa Phan
Dr. Dibya Jyoti Mondal
Sandu Yergeshbayeva
Miguel Gakiya-Teruya
Govind Sasi Kumar
Ian Campbell
Victoria Li
Shubham Bisht
Milo Adams
Samuel Adegboyega
Divya Kumar
Eduardo Hernandez
Gerald Ciani
Gia Rivers