## Slide 1
Growth of Metal Silicides from Metal Flux Reactions
Susan E. Latturner
Department of Chemistry
Florida State University
I. Metal flux synthesis
Zintl phases and Thermoelectric materials
Metal silicides A/Mg/Si (A = Ca, Sr, Ba, Eu, Yb)

## Slide 2: Metal Flux Synthesis
Common metal fluxes and products
Tin flux: PrCo2P2, BaFe2As2, Co7Zn3Sn8
Aluminum flux: Co4Al13, Y2Al3Si2, CeNiAl4Ge2, U8Al19Si6
Gallium flux: Mn123Ga137, Yb3Ga4Ge6, Tb1.8Si8C2B36
Metal flux synthesis: reaction where one low-melting metal reactant is present in large excess, acting as a solvent.
Flux synthesis advantages:
Low temperatures--kinetic/metastable products
Liquid state reaction--crystal growth
Exploratory synthesis: allows reactants to find product with local energy minimum structure

## Slide 3
Quartz tube
Crucible containing flux + reactants
Quartz wool for separation of product from flux
Metal Flux Synthesis
Combine reactants, add excess amount of suitable flux metal
Heat above mp of flux, slowly cool
Centrifuge while flux still molten
Time (hr)
Temp (°C)
Centrifuge
or cool and then etch
Unknown precipitations, phase transitions

## Slide 4
Characterization of product compounds
What’s in it?
Elemental analysis to determine what elements were incorporated
SEM-EDS
What is the structure?
Single crystal XRD to determine positioning of elements
What other products were formed?
Powder XRD to determine purity, yield
What are its properties?
Band structure calculations to explore electronic structure
Magnetic susceptibility
Thermoelectric/transport measurements

## Slide 5
Intermetallics and Zintl Phases
Intermetallic compounds: Compounds comprised of two or more metals or metalloids
Zintl phases: Subclass of Intermetallics. Compounds comprised of electropositive metal (Group 1, Group 2, some RE) and metalloid
Charge transfer between electropositive metal and electronegative metalloids leads to metal cations and metalloid anions that are charge-balanced. Causes semi-metallic or semiconducting behavior
Often have complex structures
Metal + metal metal + metalloid metal + nonmetal
Alloys Zintl phases Ionic salts
CuxNi1-x Mg2Si, Na4Sn9 MgO, NaCl
Metallic semimetal/semiconductor insulator

## Slide 6
Classifying compounds based on differences in electronegativity c
Electronegativity c = 1 – 2 for metals c = 2.5 – 4 for nonmetals

## Slide 7
Thermoelectric materials
Generate a voltage when a temperature gradient is applied
Used as: power sources (makes use of waste heat)

## Slide 8
Thermoelectric materials
To maintain thermal gradient while producing a voltage, compound must have:
Low thermal conductivity k
High electrical conductivity s (low electrical resistivity r)
High Seebeck coefficient S (voltage / DT)
Thermoelectric figure of merit:

## Slide 9
Problem: r and S are interrelated!
Best balance: Doped semiconductors/semimetals: Bi2Te3, Yb14MnSb11, PbTe. Or…Zintl phases!
k is relatively independent, make as low as possible (heavy elements, complex structure, disorder)
Thermoelectric materials

## Slide 10: Magnesium-based fluxes: Mg/Al or Mg/Zn
Adding Al or Zn lowers Mg m.p. Using 22 mmol Mg, 8 mmol of Zn or Al.
Silicon reacts with divalent metals (A = Ca, Sr, Ba, Eu, Yb) in Mg-rich melt
Large family of new A/A’/Mg/Si compounds
Charge-balanced Zintl phases
Al or Zn not incorporated into products

## Slide 11
What determines structure and composition of product?
Ionic radii of A2+ cations
Reactant ratio
Heating profile/cooling rate
Cation | Radius (Å)
Mg2+ | 0.86
Ca2+ | 1.14
Sr2+ | 1.32
Ba2+ | 1.49
Eu2+ | 1.31
Yb2+ | 1.16
Possible complication with Eu and Yb: They can be trivalent
Yb3+ radius: 1.01 Å
Eu3+ radius: 1.09 Å
Ternary A/Mg/Si products

## Slide 12
Ternary A/Mg/Si products
Mg/Zn + Si + A
Sr5+xMg19-xSi12
CaMgSi
Ba5Mg19Si12
A = Ca
A = Yb
Eu5+xMg19-xSi12
A = Eu
A = Sr
A = Ba
Yb2MgSi2
Smaller A cations: give orthorhombic TiNiSi – type product (CaMgSi) or tetragonal U3Si2 – type product (Yb2MgSi2)
Larger A cations: give hexagonal Ho5Ni19P12 – type products

## Slide 13
CaMgSi
TiNiSi type
Orthorhombic
Space group Pnma
a = 7.4690(2)Å
b = 4.4255(1)Å
c = 8.3113(2)Å
(Ca2+)(Mg2+)(Si4-)
Zintl phase, semimetal
Si anions surrounded by 9 cations
Si@(Ca/Mg)9 shown in polyhedral mode

## Slide 14
Yb2MgSi2
Mo2FeB2 type
Tetragonal
Space group P4/mbm
a = 7.0495(1)Å
c = 4.1313(1)Å
Contains Si-Si unit, formally [Si26-]
Zintl phase: (Yb2+)2(Mg2+)[Si26-]
…if the Yb is +2! Reports indicate it is Yb3+
Yb
Mg
Si

## Slide 15
A5+xMg19-xSi12 (A = Sr, Ba, Eu)
●A ●Mg ●Si ●A/Mg
compound | Cell parameters (Å)
Ba5Mg19Si12 | a = 14.6392, c = 4.4775
Sr7.82Mg16.18Si12 | a = 14.8076, c = 4.4720
Eu8Mg16Si12 | a = 14.882, c = 4.4863
Ho5Ni19P12 type
A in the Ho sites,
Mg in the Ni sites,
Si in the P sites
Hexagonal, P-62m
3f mixed site:
Smaller A2+ can mix on this Mg site (Ba2+ can’t fit)
Charge-balanced: (A2+/Mg2+)24(Si4-)12

## Slide 16
A/A’/Mg/Si semi-metallic silicides
Mg/Zn + Si + A
Sr5+xMg19-xSi12
CaMgSi
Ba5Mg19Si12
A = Ca
A = Yb
Eu5+xMg19-xSi12
A = Eu
A = Sr
A = Ba
Yb2MgSi2
What happens if you use more than one A element?

## Slide 17
A5+xMg19-xSi12 (A = Sr, Ba)
Ba mmol | Sr mmol | Product | a (Å) | c (Å) | Volume (Å3)
3 | 0 | Ba5Mg19Si12 | 14.6392(2) | 4.47754(9) | 831.00(3)
2.25 | 0.75 | Ba4.86Sr2.94Mg16.20Si12 | 14.9113(3) | 4.5507(1) | 876.27(4)
1.5 | 1.5 | Ba3.63Sr4.20Mg16.17Si12 | 14.9063(2) | 4.5382(1) | 873.28(3)
0.75 | 2.25 | Ba1.93Sr5.99Mg16.08Si12 | 14.8730(4) | 4.5082(2) | 863.64(6)
0 | 3 | Sr7.82Mg16.18Si12 | 14.8076(4) | 4.4720(1) | 849.18(5)
Different amounts of Ba + Sr reacted with 3 mmol Si in Mg/Zn flux (22:8 mmol)
All products have Ho5Ni19P12 structure type
Ba goes on Ho sites only
Sr goes on Ho sites and mixes on one Ni site
Zarei, A.; Uddin, M.S.; Baumback, R.; Wei, K.; Latturner, S.E.; Inorg. Chem., 2024, submitted.

## Slide 18
(Ba/Sr)5+xMg19-xSi12 Electronic Properties
Ba5Mg19Si12 (well ordered, no site mixing) is semiconducting with Eg = 0.02 eV.
Sr7.82Mg16.18Si12 and Ba3.6Sr4.2Mg16.2Si12 are metallic

## Slide 19
(Ba/Sr)5+xMg19-xSi12 Thermal Conductivity
Thermal conductivity is sum of electron contribution and lattice contribution ktot = kelec + klatt
kelec directly proportional to conductivity; can be calculated; subtracted from ktot to get lattice contribution
More disorder and rattling atoms  lower klatt

## Slide 20
Thermoelectric figure of merit:
Lowest for Ba5Mg19Si12
Higher for the analogs with more disorder (Sr/Mg and Sr/Ba mixing)
Need high temp measurements!
Improve zT by lowering klatt
Heavier atoms (Yb, Eu?)
More rattling (Ca mixing?)
More complex structures?
(Ba/Sr)5+xMg19-xSi12

## Slide 21
(A/A’/Mg)2Si semi-metallic silicides
Mg/Zn + Si + A
Sr5+xMg19-xSi12
CaMgSi
Ba5Mg19Si12
A = Ca
A = Yb
Eu5+xMg19-xSi12
A = Eu
A = Sr
A = Ba
Yb2MgSi2
What happens if you use more than one A element?

## Slide 22
Ba5Mg19Si12
Different amounts of Ba + Ca reacted with 3 mmol Si in either Mg/Al or Mg/Zn flux (22:8 mmol)
CaMgSi
Ca/Ba/Mg/Si (Taylor’s version)
Ca:Ba mmol amounts
3:0 2:1 1.5:1.5 1:2 3:0
CaMgSi + Ba2Ca2Mg10Si7
Ba2Ca2Mg10Si7 + Ba5Mg19Si12 type
Ba5Mg19Si12 type

## Slide 23
Ba2Ca2.3Mg9.7Si7
Si1
Si2
Si3
Si
Ba
Ca/Mg
Mg
Silsby, K.; Latturner, S.E.; Kauzlarich, S.M. Chem. Mater., 2015, 27, 6708-6716
Zr2Fe12P7 type
hexagonal, P-6; a = 11.196(2) Å, c = 4.4595(9) Å
Ba in the Zr sites, Si in the P sites, Mg in the Fe sites
Ca mixes on one Mg site

## Slide 24
Charge-balanced Zintl phase: (Ba2+/Ca2+/Mg2+)14(Si4-)7
Band structure calculations indicate semiconductor/semimetal
Chart: Partial DOS
Ba2Ca2.3Mg9.7Si7

## Slide 25
Ba2Ca2.3Mg9.7Si7 electrical properties
Chart: Temperature (K)
Increasing resistivity as temperature rises (metallic/semimetallic)
Low thermal conductivity
Chart: Temperature (K)
| 319.5 | 372.6 | 422.6 | 472.6 | 522.29999999999995 | 572.79999999999995 | 623.1 | 672.7 | 723.1 | 773 | 823 | 872.9 | 922.8 | 972.8 | 872.3 | 772.2 | 672.5 | 572.20000000000005 | 472.3 | 372.7
Thermal Conductivity SPS1 (W/(m*K)) | 2.538 | 2.429 | 2.327 | 2.221 | 2.111 | 2.025 | 1.962 | 1.908 | 1.891 | 1.913 | 1.93 | 1.975 | 2.053 | 2.178 | 1.997 | 1.961 | 2.025 | 2.141 | 2.267 | 2.442
Silsby, K.; Kauzlarich, S.M.; Latturner, S.E. Chem. Mater., 2015, 27, 6708-6716

## Slide 26
Ba2Ca2.3Mg9.7Si7 thermoelectric properties
High Seebeck coefficient; n-type
Chart: Temperature (K)
Chart: Temperature (K)
| 323 | 373 | 423 | 473 | 523 | 573 | 623 | 673 | 723 | 773 | 823 | 873 | 923 | 973 | 873 | 773 | 673 | 573
ZT | 0.018996 | 0.033079 | 0.051562 | 0.07613 | 0.1079 | 0.14619 | 0.19123 | 0.24302 | 0.29506 | 0.34256 | 0.38442 | 0.41785 | 0.44065 | 0.44825 | 0.41367 | 0.32717 | 0.2232 | 0.13147
ZT = S2T/rk
Maximum of 0.4 at 900 K
Improvements likely if substituted or doped

## Slide 27
Flux reactions enable crystal growth of metal silicides
Semi-metallic silicide Zintl phases show promise as thermoelectric compounds
Improve zT by lowering klatt
Heavier atoms (Yb, Eu?)
More disorder (site mixing)
Rattling of small cations mixed on large cation sites
More complex structures?
zT likely higher at high temperature; need high temp measurements!
Conclusions / Future Work

## Slide 28
Acknowledgments
Xiaowei Ma, Kurt Silsby, Milorad Stojanovic, Jeff Whalen, Guillermo Vasquez, Jo Haddock, Olufemi Araoyimbo, Amir Zarei, Taylor Walker
Susan Kauzlarich (UC Davis)
Kaya Wei and Ryan Baumbach (NHMFL)

## Slide 29
Compound | Structure type | Space group | Unit cell parameters (Å)
Ba1.9Ca2.4Mg9.7Si7 | Zr2Fe12P7 | P-6 | a = 11.196(2) c = 4.4595(9)
Ba2Yb0.88Mg11.12Si7 |  |  | a = 11.0830(6) c = 4.4150(3)
Eu2Yb1.11Mg10.89Si7 |  |  | a = 10.9910(7) c = 4.3250(3)
Sr5Mg19Si12 | Ho5Ni19P12 | P-62m | a = 14.457(1) c = 4.3713(4)
Ba5Mg19Si12 |  |  | a = 14.5874(8) c = 4.4662(2)
Eu7.5Mg16.5Si12 |  |  | a = 14.668(5) c = 4.428(1)
Ba5Eu2.85Mg16.15Si12 |  |  | a = 14.857(2) c = 4.5225(5)
Ba3.4Sr4.5Mg16Si12 |  |  | a = 14.862(9) c = 4.521(2)
Sr4.8Ca3.2Mg16Si12 |  |  | a = 14.666(2) c = 4.4187(7)
Ba5Yb2.26Mg16.73Si12 |  |  | a = 14.8223(8) c = 4.5174(3)
Eu5Yb2Mg17Si12 |  |  | a = 14.526(2) c = 4.3800(6)
Sr5Eu1.39Mg17.61Si12 |  |  | a = 14.553(2) c = 4.4102(7)
Ba6Yb1.84Mg18.16Si13 | Zr6Ni20P13 | P-6 | a = 15.455(1) c = 4.5046(3)
Ba6Eu3Mg17Si13 |  |  | a = 15.482(1) c = 4.5082(3)
Ba20Yb4.7Mg61.3Si43 | Ho20Ni66P43 | P63/m | a = 27.928(4) c = 4.4808(6)
Ba20 Eu5.6Mg60.4Si43 |  |  | a = 27.988(3) c = 4.4915(6)
Ba20Mg66Si43 |  |  | a = 27.805(4) c = 4.4741(6)
Large family of (A/A’/Mg)2Si from flux growth