## Slide 1
Research Experience for Undergraduates, FSU 2019
Metal Chalcogenides for Fun and Profit
Susan E. Latturner
Department of Chemistry
Florida State University
Inorganic extended solids
Band structure basics
Metal chalcogenides
Flux growth

## Slide 2
Inorganic Extended Solids: Crystal structure
Organic compounds: focus is on discrete molecular units
Interactions between the molecules not important
Inorganic extended solids: atoms are bonded in infinite 3-D array
Pattern of repeating unit cells pack together to fill space
    Size, symmetry of unit cell and position of atoms in it = crystal structure
Cu3VSe4
Cubic
P ͞4 3 m
a = 5.5636(5) Å
MoSe2
Hexagonal
P 63/m m c
a = 3.2880 Å
c =12.9000 Å

## Slide 3
Unit cell

## Slide 4
Seven Crystal Systems
Cubic
Tetragonal
Orthorhombic
Hexagonal
Trigonal/Rhombohedral*
Monoclinic
Triclinic

## Slide 5
ZnS
Zinc blende / Sphalerite
Half of tetrahedral sites filled
cubic, F4-3m
a = 5.406Å
Structures derived from ccp (fcc) layers of anions

## Slide 6
ZnS, Wurtzite
Half of tetrahedral sites filled
hexagonal, P63mc
a = 3.811Å, c = 6.234Å
High temperature form
Structures derived from hcp packing of anions

## Slide 7
Crystal structure
Zinc Selenide, ZnSe
Space group F4-3m
a = 5.633 Å
CuGaSe2
Tetragonal
Space group I-42d
a = 5.614 Å
c = 11.022 Å
Take “Zn2Se2” and substitute Cu+ and Ga3+ for Zn2+ cations. Cu and Ga siting on the Zn sites is not random; “coloring pattern” lowers symmetry from cubic to tetragonal, doubling one of the axes

## Slide 8
Band Structure
For an extended solid the band structure plays the same role that an MO diagram does for a molecule.
Band structure is the link between crystal structure, bonding and properties.
Electronic conductivity
Optical properties, including absorbance
Electronically driven structural distortions
Magnetic Properties of Metals
Catalytic Activity

## Slide 9
Molecular orbitals vs bands
Positioning and spatial overlap of atomic orbitals in an ordered crystalline material will result in bonding and band formation.
An extended 3-D version of what happens in a molecule
Molecule: atomic orbitals interact to form stabilized bonding molecular orbitals and higher energy antibonding MO’s
Bulk solid: millions of atomic orbitals interact to form “crystal orbitals” that extend through the entire crystal. These crystal orbitals are grouped into bands.

## Slide 10
W.D. Callister, Materials Science and Engineering: An Introduction
From atom to many atoms
When 12 atoms aggregate, their atomic orbitals interact to form bonding and antibonding states

## Slide 11
Density of States—bulk material
Bands form as atoms go from well-separated to packed together in a bulk solid at their stable equilibrium positions
Millions of atoms → millions of crystal orbitals or “states” packed into energy bands

## Slide 12
Density of States
Metals: no bandgap between filled and unfilled states
Semiconductors: bandgap; Eg between 0 – 4 eV
Insulators: large bandgap; Eg > 4 eV
Filled states
Empty states

## Slide 13
Density of States of Silicon
Empty states (conduction band, CB)
Filled states (valence band, VB)
Band gap (Eg)
Fermi level (EF)

## Slide 14
Material | Band gap (eV)
InAs | 0.4
Ge | 0.67
GaSb | 0.7
Si | 1.11
InP | 1.34
GaAs | 1.43
CdSe | 1.74
SnS2 | 2.2
CdS | 2.42
ZnSe | 2.8
TiO2 | 3.0
GaN | 3.37
ZnS | 3.6
Diamond | 5.46 - 6.4 eV
Band gaps of semiconductors
(insulator)

## Slide 15
Color in Extended Inorganic Solids
Intratomic (Localized) excitations—isolated TM ions in solids
Cr3+ Gemstones (i.e. Cr3+ in Ruby and Emerald)
Blue and Green Cu2+ compounds (i.e. malachite, turquoise)
Blue Co2+ compounds (i.e. Al2CoO4, azurite)
Charge-transfer excitations (metal-metal, anion-metal)
Fe2+ → Fe3+ in Prussian Blue
O2- → Cr6+ in BaCrO4
Valence to Conduction Band Transitions in Semiconductors
WO3 (Yellow)
CdS (Yellow) & CdTe (Black)
HgS (Cinnabar - Red)

## Slide 16
Electromagnetic Radiation and the Visible Spectrum
UV 100-400 nm 12.4 - 3.10 eV High energy
Violet 400-425 nm 3.10 - 2.92 eV
Blue 425-492 nm 2.92 - 2.52 eV
Green 492-575 nm 2.52 - 2.15 eV
Yellow 575-585 nm 2.15 - 2.12 eV
Orange 585-647 nm 2.12 - 1.92 eV
Red 647-700 nm 1.92 - 1.77 eV
Near IR 10,000-700 nm 1.77 - 0.12 eV Low energy

## Slide 17
Color of a material = color reflected from it into our eyes
Color reflected = color not absorbed
Emission is a different process (observing energy emitted by a material that is going from excited state to ground state)
If absorbance occurs in one region of the color wheel the material
appears with the opposite (complimentary color). For example:
material absorbs violet light → Color = Yellow
material absorbs red light → Color = Green
material absorbs violet, blue & green → Color = Orange-Red
material absorbs red, orange & yellow → Color = Blue

## Slide 18
Absorption spectra of molecular species
Discrete energy levels lead to narrow peaks

## Slide 19
Absorption spectra of crystalline semiconductors
Transition between valence band states and conduction band states leads to broad absorbance
(filled states)
(empty states)

## Slide 20
Wavelength (nm)
absorbance
300 400 500 600 700
Color of semiconductors
Eg > 3 eV white
Eg < 1.5 eV black
In between: yellow, orange, red

## Slide 21
HgS, cinnabar
(Eg = 2.0 eV)
Vermilion pigment
Red tattoo ink
PbS, galena
(Eg = 0.37 eV)
Eyeliner/kohl
Ancient metal sulfide pigments

## Slide 22
Metal sulfide pigments
Cadmium-based pigments used from Impressionist era to today
Cadmium yellow (CdS)
Cadmium orange (CdS1-xSex)
Cadmium red (CdSe1-xSx)

## Slide 23
Bandgap Engineering
Control of band gap by substitution of one ion for another
Isovalent substitution (same charge ion)
CdS Eg = 2.42 eV CdSe Eg = 1.74 eV
CdS1-xSex Eg = 1.74 to 2.42 eV, depending on x
CuGaSe2 Eg = 1.7 eV CuInSe2 Eg = 1.0 eV
CuIn1-xGaxSe2 Eg = 1.0 to 1.7 eV, depending on x
Aliovalent substitution (substituted ion has different charge)
    Can substitute higher and lower valent cations simultaneously to balance charge, but they may order and change structure.
(ZnSe)2 → CuGaSe2

## Slide 24
(anion states)
(cation states)
Shifting band energies
CdS Eg = 2.42 eV
CdSe Eg = 1.74 eV
CdS1-xSex Eg dep on x

## Slide 25
CdS (Eg = 2.45 eV) CdSe (Eg = 1.74 eV) CdTe (Eg = 1.45 eV)
ZnS (Eg = 3.6 eV) ZnSe (Eg = 2.8 eV)
The above items are carefully grown single crystals of ZnS or ZnSe which have been cut into shapes. A lot of solar cell engineering involves growth of large crystals or deposition of single crystalline films.

## Slide 26
Band gap engineering
Controlled modification of band gap energy by substitution of one element for another in a compound
Vegard’s law—Eg should be directly proportional to substitution amount

## Slide 27
Bandgap Engineering in CIGS
Cu(In/Ga)S2 and Cu(In/Ga)Se2

## Slide 28
CIGS: Cu(In/Ga)Se2
Excellent absorber (thin films sufficient to product good photocurrent from sunlight)
Band gap tailorable in the most intense region of sunlight (1 – 1.5 eV)

## Slide 29
Solar cells
Materials for use in solar cells absorb part of the light emitted by the sun
This causes an e- to go from a low energy orbital/state to a higher energy orbital/state
This excited electron and the hole where it used to be must then separate (go to opposite sides of the device)—this occurs at a junction in the device
Thus the absorbance of light will produce a voltage (due to separated e- and h+): photovoltaic

## Slide 30
The solar radiation spectrum
Light emitted by the sun in a broad range of energies
Enough sunlight hits the earth every hour to power the world’s economy for a year.

## Slide 31
Silicon-based solar cell
Silicon (indirect gap 1.1 eV)
Sufficient thermal energy enables photovoltaic behavior despite inefficient absorbance. Cells must be fairly thick. (Direct-gap absorbers such as CIGS or CdTe can function in thin-film form.)

## Slide 32
Eg (CdS) = 2.45 eV
Eg (CdTe) = 1.45 eV
CdS/CdTe solar cell

## Slide 33
When price is no object:
III-V multijunction photovoltaics
Direct gap and ability to tailor band gap energy allows for multijunction solar cells (also known as tandem cells) which use more of the solar spectrum more efficiently (less loss of excess photon energy by waste heat)
Each junction has a different energy gap, will use a different part of spectrum
Outermost junction = largest gap; smaller gaps as you go deeper

## Slide 35
Solar cell material efficiencies
Most efficient materials are semiconducting inorganic extended solids
Excellent properties due to crystallinity and band structure

## Slide 36: Flux Synthesis of Metal Chalcogenides
Common metal fluxes and products
Tin flux: PrCo2P2, Co7Zn3Sn8
Aluminum flux: Co4Al13, Y2Al3Si2, CeNiAl4Ge2
Gallium flux: Mn123Ga137, Yb3Ga4Ge6, Tb1.8Si8C2B36
Reactivity of the flux toward solutes varies
  Reactive solvent – flux element incorporated into the growing crystalline phase
  Unreactive solvent – not incorporated into the product
Flux synthesis: reaction where one low-melting elemental reactant is present in large excess, acting as a solvent.

## Slide 37
Fluxes of interest
Element m.p. (°C)
Ga 29.8
S 115
In 157
Sn 232
Bi 271
Zn 419

## Slide 38
Flux Reactions
Flux synthesis advantages:
Low temperatures--kinetic/metastable products
Liquid state reaction--crystal growth
Exploratory synthesis: allows reactants to find product with local energy minimum structure
Mixed fluxes:
Lowered melting points
Can dissolve wider range of reactants

## Slide 39
Quartz tube
Reactants and flux
Quartz wool for separation of product from flux
Flux Synthesis
Combine reactants, add excess amount of suitable flux
Heat above mp of flux, slowly cool
Centrifuge while flux still molten
Time (hr)
Temp (°C)
Centrifuge
or cool and then etch

## Slide 40
Objective
Synthesize AxMySz with band gap of 1 – 2 eV
Need: charge-balancing (A2+ and Mn+ cations / sulfide anions)
ability to do isovalent substitution
air-stability
sufficient yield for measurements
BaxMySz or CaxMySz or ZnxMySz
Explore different M (M = Ga, In, Sn, Bi)
React BaS or CaS or Zn with S in excess M flux
or
React BaS or CaS or Zn with M in excess sulfur flux

## Slide 41
Sulfur flux growth of Ba/(Sb,Bi)/S phases
BaS + Sb in excess sulfur flux  BaSb2S4 (monoclinic, red powder; Eg = 1.6 eV)
BaS + Bi in excess sulfur flux  BaBi2S4 (hexagonal, black powder; Eg = 1.2 eV)
BaS + Sb and Bi in excess sulfur flux  Ba(Sb1-xBix)2S4
with 0 < x < 0.3 at which point structure changes

## Slide 42
Ba
Sb
S
Bandgap of 1.6 eV will shrink as Sb is substituted by Bi
Confirmed by UV/Vis/NIR spectroscopy

## Slide 43
Metal flux allows higher temperatures
BaS / S / M flux
Need high enough temperature for BaS, S, MxSy to react; crystal growth
Possible sulfur vapor pressure?
Canfield et al. found ratio up to S40Bi60 can be heated up to 1000 °C without rupturing tube or detectable evaporation of S

## Slide 44
BaS + S in excess M flux
Possible products
BaS / S / Bi
a-BaBi2S4, b-BaBi2S4
BaS / S / Sn
BaSnS2, Ba3Sn2S7, BaSn2S3, Ba2SnS4, Ba7Sn3S13, Ba12Sn4S23, Ba7Sn5S15, BaSn2S5, Ba6Sn7S20, Ba8Sn4S15, BaSn3S4, BaSnS3
BaS / S / Ga
BaGa4S7, Ba2Ga2S5, Ba5Ga2S8, Ba4Ga2S7, Ba3Ga2S6, Ba4Ga2S8, BaGa2S4
BaS / S / In
BaIn2S4, Ba2In2S5, Ba12In4S19, Ba4In2S8

## Slide 45
Indium flux reactions
BaS + S in excess of indium metal (1:1:10 mmol ratio)
Product targeted: BaIn2S4
Allows for substitution on several sites to modify Eg
Unfortunately, InS forms very readily!

## Slide 46
Wide variety of binary and ternary chalcogenides with potentially useful properties
Semiconducting compounds of potential interest as solar cell materials, pigments, LED’s
Considerations that need to be balanced for solar cells:
Efficiency of cell
Price of processing/purity needed
Abundance of elements
Toxicity of elements
Making these materials nanosized (quantum dots) is also a huge field (Strouse, et al.)!
Final thoughts on metal chalcogenides