## Slide 1
Kenneth Hanson
Department of Chemistry & Biochemistry
Florida State University, Tallahassee, FL, USA
Understanding and Controlling Molecular Excited State Processes Using Metal Oxide Interfaces

## Slide 2
Molecular Photochemistry/Photophysics
Molecule
phosphorescence
fluorescence
internal
conversion
intramolecular charge transfer
electron transfer
proton transfer
energy transfer
excimer formation
exiplex formation
photochemical transformation
hn
conformational change

## Slide 3
Molecular Photochemistry/Photophysics
Sundström et al. J. Phys. Chem. B 1999, 103, 2327-2346.
Lundholm et al. RSC Adv. 2014, 4, 25502-25509.
Energy Transfer
Electron Transfer

## Slide 4: Structural Control: Humans
Kent et. al. J. Am. Chem. Soc., 2010, 132, 12767
Ma et. al. Nature Protocols, 2013, 8, 439
Phospholipid Bilayers
Metal Organic Frameworks
Polypeptides
Slate et. al. J. Am. Chem. Soc., 1998, 120, 4885
Crystals
Zhu et. al. J. Phys. Chem. C, 2014, 118, 14150

## Slide 5: Metal Ion-Linked Multilayer
NanoMO2
Energy/e- Cascade
Control e- Transfer
Singlet Fission
Photon Upconversion
5

## Slide 6
hn → hn
hn → hn
hnex
S1
S2
S0
S3
IC
IC
hnem
Down Conversion vs. Upconversion

## Slide 7
hn
T1
Annihilator
Sensitizer
S1
T1
S1
S0
(1)
(2)
(3)
(4)
(5)
hn
T1
Annihilator
S1
T1
Sensitizer
S1
S0
2 hn → hn
Photon Upconversion

## Slide 8
(4)
(5)
hn
T1
S1
T1
S1
S0
2 hn → hn
Photon Upconversion
Annihilator
Sensitizer

## Slide 9
Sensitizer-Annihilator Interactions
Solution
MOF
Polymer Films
Neat-solvent
JACS 2013, 135, 19056
JACS 2016, 138, 6541
JACS 2007, 129, 12652
Chem. Commun., 2004, 2860
Photochem. Photobiol. Sci. 2014, 13, 48
Microemulsion
J. Phys. Chem. C, 2013, 117, 14493
Heterogeneous

## Slide 10
Solar Cell Efficiency
Standard solar cell ~33%
Max Theoretical Efficiency
Schulze and Schmidt Energy Environ. Sci. 2015, 8, 103-125
1.3 eV bandgap
Pin = 100 mW/cm2 (AM1.5)
Pmax = J x V
Voc
Large BG
High V, Low J
Small BG
Low V, High J
SQ Limit
1.3 ev
hn
hn
hn
hn
Voc

## Slide 11
Solar Cell Efficiency
Standard solar cell ~33%
Max Theoretical Efficiency
Schulze and Schmidt Energy Environ. Sci. 2015, 8, 103-125
1.3 eV bandgap
Solar cell with upconversion > 45%
1.76 eV bandgap
with TTA-UC
Perovskites, OPV, DSSC
Ekins-Daukes and Schmidt,
Appl. Phys. Lett., 2008 93, 063507.

## Slide 12
Harnessing TTA-UC
J. Phys. Chem. Lett. 2013, 4, 2073.
Chem. Commun. 2012, 48, 209.
hn
hn
Transmission
Light absorption and TTA
Upconverted emission
Absorption by a solar cell
(3)
Solar Cell
(4)
S
A*
A
Upconversion Solution/Film
(2)
(1)
Optical Coupling:

## Slide 13
Harnessing TTA-UC
hn
hn
Transmission
Light absorption and TTA
Upconverted emission
Absorption by a solar cell
(3)
Solar Cell
(4)
S
A*
A
Upconversion Solution/Film
(2)
(1)
Optical Coupling:
No isotropic emission
No self-absorption
Increase sensitizer concentration
Electronic Coupling:
Light absorption and TTA
Photocurrent Generation
S
A*
A
Upconversion Solar Cell
(1)
(2)
e-
Need A* at a charge separation interface!
hn

## Slide 14: Metal Ion-Linked Multilayer
NanoMO2
Hill et al. J. Phys. Chem. Lett. 2015, 6, 4510.
S and A in proximity
A-A interactions
On a charge separation interface
Easy DSSC integration

## Slide 15: Metal Ion-Linked Multilayer
NanoMO2

## Slide 16: TTA-UC Emission
lex = 532 nm (1 W/cm2)
Hill et al. J. Phys. Chem. Lett. 2015, 6, 4510.
Φ = 0.0023

## Slide 17: TTA-UC Emission
Hill et al. J. Phys. Chem. Lett. 2015, 6, 4510.
Castellano et al. J. Phys. Chem. Lett. 2012, 3, 299-303.
Strong TTA Limit
Weak TTA Limit
Slope = 1
Slope = 2

## Slide 18: Mechanism
T1
S1
ISC
S0
ET
hn
S1
ZrO2
CB
VB
T1
E
S0
S
Zn
A
e-
T1
S1
ISC
S0
ET
hn
S1
TiO2
CB
VB
T1
S0
S
Zn
A
hn
Upconverted Emission!
Photocurrent?
e-
e-
D/D+
e-

## Slide 19
TTA-UC Photocurrent
J. Phys. Chem. Lett. 2015, 6, 4510.
On ZrO2: Upconverted Emission
On TiO2: Upconverted Photocurrent
λex = 532 nm
TiO2-ML
Co(bpy)32+/3+
MeCN
V
ZrO2-ML
MeCN
Pt counter electrode

## Slide 20
TTA-UC Photocurrent
On TiO2: Upconverted Photocurrent
TiO2-ML
Co(bpy)32+/3+
MeCN
V
Pt counter electrode
Jsc/Voc greater than the sum of its parts.
Jsc= 0.009 mA/cm2
Demonstrated an integrated TTA-UC solar cell.
h = 1.6 x 10-5 %
ACS Energy Lett. 2016, 1, 3-8.

## Slide 21
Increasing UC Photocurrent (JUC)
JPC Lett., 2018, 9, 5810
9 mA/cm2
ACS Energy Lett. 2016, 1, 3-8.

## Slide 22
Increasing UC Photocurrent (JUC)
JPC Lett., 2018, 9, 5810
9 mA/cm2
ACS Energy Lett. 2016, 1, 3-8.
J. Mater. Chem. A, 2017, 5, 11652-11660.
78 mA/cm2

## Slide 23
Increasing UC Photocurrent (JUC)
JPC Lett., 2018, 9, 5810
158 mA/cm2
JACS 2017 , 139, 10988.

## Slide 24
Increasing UC Photocurrent (JUC)
JPC Lett., 2018, 9, 5810
315 mA/cm2
ACS Energy Lett. 2019, 4, 1458.
158 mA/cm2
JACS 2017 , 139, 10988.

## Slide 25
Increasing UC Photocurrent (JUC)
JPC Lett., 2018, 9, 5810
29 mA/cm2
ACS Appl. Energy Mater. 2020, 3, 29.

## Slide 26
Increasing UC Photocurrent (JUC)
JPC Lett., 2018, 9, 5810
12 mA/cm2
JPC C 2020, 43, 23597.
29 mA/cm2
ACS Appl. Energy Mater. 2020, 3, 29.

## Slide 27
Increasing UC Photocurrent (JUC)
JPC Lett., 2018, 9, 5810
3.5 mA/cm2
12 mA/cm2
JPC C 2020, 43, 23597.
JMC C 2022, 10, 4947.
29 mA/cm2
ACS Appl. Energy Mater. 2020, 3, 29.

## Slide 28
Increasing UC Photocurrent (JUC)
JPC Lett., 2018, 9, 5810
ACS AM&I 2021, 13, 32601.
Performance Limitations:

## Slide 29
Energy and Electron Transfer
Upconversion Trilayer
Triplet Sensitizer
Annihilator
e- Acceptor
Singlet Sensitizer
1A
3A*
1A*
1S
3S*
1S*
1F*
1F
kET1
kex(F)
kex(S)
γTTA
kr(F*)
knr(F*)
ket
kBTET
3F*
ket
kBET2
TiO2
Glass
ACS Energy Lett. 2019, 4, 6, 1458
kBET1
kinj(1A*)
kinj(3A*)
kBeT1
kBeT2
kISC
kTET
kr(1A*)
knr(1A*)
knr(3A*)
kr(3S*)
knr(3S*)
kinj(S*)
kmig

## Slide 30
Energy and Electron Transfer
Photosynthesis
Triplet Sensitizer
Annihilator
e- Acceptor
Singlet Sensitizer
1A
3A*
1A*
1S
3S*
1S*
1F*
1F
kET1
3x1011
kex(F)
>1015
kex(S)
>1015
γTTA
1.0x10-15
kr(F*)
5.9x108
knr(F*)
5.8x108
ket
<106
kBTET
~0
3F*
ket
<106
kBET2
4.4x109
TiO2
Glass
ACS Energy Lett. 2019, 4, 6, 1458
kBET1
1.9x107
kinj(1A*)
4.5x1011
kinj(3A*)
1.6x106
kBeT1
9.5x106
kBeT2
5.5x106
kISC >1012
kTET
1.3x104
kr(1A*)
2.5x108
knr(1A*)
2.3x108
knr(3A*)
4.9x103
kr(3S*)
2.5x102
knr(3S*)
1.7x104
kinj(S*)
1.6x106
kmig
Upconversion Trilayer
https://doi.org/10.48550/arXiv.1608.06913

## Slide 31: Metal Ion Linked Multilayer Structure
Energy/Electron Transfer Cascade
ACS AM&I 2016, 8, 28633
Water Oxidation DSPEC
ACS Omega, 2017, 2, 3901.
H2 Generation
Chem. Sci. 2021, 12, 50.
Molecular Rectifiers
Angew. Chemie. 2018, 57, 15390.
ACS Appl. Opt. Mater. 2023, 1, 1156.
Notes: Kato out of Hokkaido University

## Slide 32: Bilayer Structure
What is known:
Not co-deposition
Metal-ion coordination
Directional E/e- transfer
What is not known:
Surface binding angle
Relative orientation
Controllability

## Slide 33: Polarized Attenuated Total Reflectance
ITO coated glass substrate
monolayer
Evanescent wave
John Thomas Bradshaw , A. PhD. Dissertation, University of Arizona, 2005
Prof. Scott Saavedra at UofA
Measure ATE and ATM
Dichroic ratio
Calculate mean tilt angle

## Slide 34: Metal Oxide-Anthracene Structure
S1
ZrO2, Al2O3
CB
VB
E
S0
e-
CB
TiO2
ITO
ITO
30o
TiO2
38o
ZrO2
37o
Al2O3
44o
1.1±0.3nm
2.2±0.5nm
1.2±0.4nm
0.5±0.1 nm
Roughness:
e-
e-
@0 nm roughness, tilt angle = 22o
Rowlen et al. JPC C 1999, 103, 1525.

## Slide 35: Metal Oxide-Anthracene Structure
S1
ZrO2, Al2O3
CB
VB
E
S0
e-
CB
TiO2
ITO
ITO
30o
TiO2
38o
ZrO2
37o
Al2O3
44o
1.1±0.3nm
2.2±0.5nm
1.2±0.4nm
0.5±0.1 nm
Roughness:
ITO
30o
ITO
31o
PO3H2 vs COOH
e-
e-
Similar angle regardless of metal oxide.
Binding group does not change the angle.
JPC C 2023, 127, 2705

## Slide 36: Multilayer Structure
ITO
ITO
Zn
31o
38o
37o
ITO
ITO
33o
Zn
One possible structure.
ITO
Zn
Zn
39o
40o
75o
Langmuir 2023, 39, 10670.

## Slide 37: Multilayer Structure
Azimuthal Angle
Is the angular measurement in a spherical coordinate system which represents the horizontal angle from a frame of reference (usually North).
ITO
Zn
Zn
39o
40o
75o
Can determine structure if we know the angle between the chromophores!

## Slide 38: FRET and Structure
Lakowicz, J.R. Principles of Fluorescence Spectroscopy, 3rd ed; Springer Science: New York 2006
J = overlap integral
= fluorescence QY of D
n= refractive index
κ2= orientation factor
r = distance
r
A
D
A
θA
θD
θT
κ2= (cos θT – 3 cos θD cos θA)2
Acceptor
r
Donor
FRET

## Slide 39: FRET and Relative Orientation
P1
P2
P3
λEx=360 nm
FRET

## Slide 40: FRET and Relative Orientation
P1
P2
P3
λEx=360 nm
FRET
A*
P*
P*
Sample | t (ps) | FFRET
ZrO2-A-Zn-P1 | 38 | 99%
ZrO2-A-Zn-P2 | 41 | 99%
ZrO2-A-Zn-P3 | 175 | 97%
Transient Absorption
J = overlap integral
= fluorescence QY of D
n= refractive index
κ2= orientation factor
r = distance
J, FD, and n are known/the same.
Use change in r/E to find k2.
(assumes constant k2 for P1-3)

## Slide 41: Polarized ATR
ITO coated glass substrate
monolayer
Evanescent wave
Both k2 and r are changing.
This method will not work.
Also, this is only one possible orientation!

## Slide 42: Porphyrin Orientation
θA
Cory Ruchlin, McGill
Former FSU UG
θP
θD
θrot
θN

## Slide 43: Porphyrin Orientation
Cory Ruchlin, McGill
Former FSU UG
θP
θD
θrot
θN

## Slide 44: Porphyrin Orientation
A vector
Porphyrin centroid
Axial dipole
Transverse dipole
Theoretical FRET Efficiency
Black lines:
Theory agrees with experiment.
Possible porphyrin orientation.
Still not a unique answer.

## Slide 45: Porphyrin Orientation
Theoretical FRET Efficiency
Possible orientation.
Not a unique answer.

## Slide 46: Porphyrin Orientation
Old Bilayer
New Bilayer
One transition dipole moment.
Is a fluorescent FRET acceptor.

## Slide 47: Emission Anisotropy
360 nm
530 nm
440 nm
hn
hn
hn
FRET

## Slide 48: Emission Anisotropy
360 nm
530 nm
445 nm
hn
hn
hn
FRET
β
Nat. Commun. 2021, 12, 2541.

## Slide 49: Emission Anisotropy
NanoMO2
A
Zn
Bo
ZrO2-A-Zn-B

## Slide 50: Emission Anisotropy
NanoMO2
A
Zn
Bo
ZrO2-A-Zn-B
ZrO2-A
ZrO2-B

## Slide 51: Emission Anisotropy
360 nm
440 nm
Emission Spectra

## Slide 52: Emission Anisotropy
360 nm
440 nm
450 nm
530 nm
Emission Spectra

## Slide 53: Emission Anisotropy
360 nm
440 nm
Emission Spectra
450 nm
530 nm
360 nm
440 nm
530 nm
FRET

## Slide 54: Emission Anisotropy
360 nm
440 nm
Emission Spectra
450 nm
530 nm
360 nm
440 nm
530 nm
FRET
Excitation Spectra (575 nm emission)

## Slide 55: Emission Anisotropy
360 nm
440 nm
Emission Spectra
450 nm
530 nm
360 nm
440 nm
530 nm
FRET
Excitation Spectra (575 nm emission)

## Slide 56: Emission Anisotropy
360 nm
445 nm
530 nm
FRET
G = IHV/IHH
r =
r = ro ()
= 37.5°
ro = 0.4 ()

## Slide 57: Bilayer Structure
37.5°
= 37.5°

## Slide 58: Bilayer Structure
Emission Anisotropy
+
Polarized ATR
=
The Average Structure
?
= 37.5°
Q = ?

## Slide 59: Polarized Attenuated Total Reflectance
Prof. Scott Saavedra at UofA:
Retired Summer 2023
FSU Spectroscopy User Facility
DMR-EPM-2327754

## Slide 60: Ongoing/Future Work
Deformation Coordinates
Energy
hn
S0
S1
Anisotropy/Polarized ATR
Ultrafast Transient Polarized ATR
Saavedra (unpublished)
Inhibiting Distortion
hn
Deformation Coordinates
Energy
S0
S1

## Slide 61: Inhibiting Distortion
J. Phys. Chem. A 2015, 119, 13, 3181–3193
hn
hn
t = 90 ns
F = 0.04%
t = 2800 ns
F = 6.3%
Steric Bulk
Strategic Surface Binding

## Slide 62: Decay Kinetics
1
2

## Slide 63: Strategic Surface Binding
1
3
t = ×5
t = ×20

## Slide 64: Conclusions
TTA-UC Emission
  On ZrO2: Blue to green upconversion
  Quadratic to Linear Behavior
TTA-UC Solar Cell
  Improvements with component selection
  JUC up to 315 mA/cm2
  Structure matters
Determine Structure (polarized ATR)
  1st layer orientation is MOx independent
  2nd layer dependent on metal and binding group
  Reasonable agreement between ATR and Theory (MM)
Efforts to Control Structure are Underway

## Slide 65: Other Research Efforts
Z-Scheme H2 Generation
J. Am. Chem. Soc. 2022, 144, 21568
Photomechanical Polymers
ACS Appl. Polym. Mater. 2022, 4,4081
Photochemical Separations
Chem. Commun. 2018, 54, 7507
J. Chem. Educ. 2023, 9, 3454.
J. Chem. Educ. 2021, 98, 5, 1529.
Chem. Ed. Research
J. Chem. Educ. 2024, ASAP.

## Slide 66
Every other Wed. 8-11 pm ET

## Slide 67
Wed. July 3rd, 8-11 pm ET
Ask_a_Scientist_Gaming on Twitch.tv
Games: Double Dragon
Contra
Super Mario Bros. NARC
Guest:
Prof. Bin Ouyang
(Chemistry & Biochemistry)
Expertise:
Computational chemistry
Machine learning
Energy storage materials

## Slide 68: Acknowledgements
  Not Pictured Contributors
  Dr. Ashley Arcidiacono (Uchicago, Postdoc)
  Dr. Suli Ayad
    (TCC, Prof.)
  Cory Ruchlin (McGill, Grad)
  Sarah Lindbom
  Luke Jodoin
  Collaborators
  Dr. Raaj Winfred (FSU)
  Dr. Igor Alabugin (FSU)
  Nikolas R. Dos Santos (FSU)
  Dr. Scott Saavedra (UA)
  Dr. Brooke Massani (UA)
  Dr. Bünyemin Çoşut (Gebze Tech)

## Slide 69: Questions?
@HansonFSU