## Slide 1: Microwave-Specific Effects on Gas-Carbon Reactions
A.E. Stiegman
Department of Chemistry and Biochemistry
Florida State University
Tallahassee, FL

## Slide 2
Our Early Efforts in Microwave Chemistry Were Inauspicious

## Slide 3
Microwaves
The frequency range for the microwave region is typically designated as occurring from 0.3 GHz and 300 GHz (1 mm to 1 m).
Microwave heating of materials, solids and liquids, takes place a fixed frequency of 2.45 GHz corresponding to a wavelength of 12.25 cm.

## Slide 4
Microwaves and Matter
The absorption of microwave radiation by molecules and solid materials is a relaxation phenomenon.
At the energy of microwave radiation there are no known resonant absorption processes that can lead to chemical processes; bond making and bond breaking.
Resonance vs Relaxation Processes

## Slide 5: Absorption of Radiation

## Slide 6: Microwave Heating in Homogeneous Solutions
Debye Theory of dipole interactions with electromagnetic radiation.
The oscillating electric field couples with the dipole moment.
This results in a torque on the molecule.
In a condensed medium, the oscillating molecule is collides with neighboring molecules which impede the relaxation.
  The molecule oscillation is out of phase with the radiation. This is a loss process that generates heat.
The average power converted to heat

## Slide 7
Microwave Heating in Homogeneous Solutions
Dielectric Spectrum of Water
A key parameter that describes these systems in the relaxation time (t) which is a measure of how long the perturbed molecule takes to recover.
Relationship to molecular properties

## Slide 8
Dielectric Loss Processes in Solids
Mechanisms for Dielectric loss in Solids
Conduction Loss
Space-Charge Recombination
Defect and Impurity Centers

## Slide 9
Debye Heating of surface dipoles.
Heating through space-charge recombination.

## Slide 10: Dielectric Spectra and Microwave Heating of Carbon
Loss tangent=0.18(±0.02)

## Slide 11
Microwaves and Heterogeneous Chemical Reactions
Our hypothesis was that selective heating of the catalyst and not the entire reaction can potentially represent a significant savings in energy.

## Slide 12: Carbon Gasification Reactions
H2O + C D CO + H2 ΔH=+131 kJ/mol 1.
CO2 + C D 2CO ΔH=+172 kJ/mol 2.
CO + H2O D 2H2 + CO2 ΔH=-41 kJ/mol 3.
2H2 + C D CH4 ΔH=-75 kJ/mol 4.

## Slide 13: Studies of the Boudouard Reaction: CO2 + C D 2CO

## Slide 14: Experimental Protocol: Kinetic Experiments
High temperature activated charcoal
Surface area: 992 m2/g
Pore Volume: .236 cm3/g
Average Pore Size: 3.25 nm
Flow: 0.5 g, 11 mm diameter, flow rate for CO2 50 mL/min
Static: 1.0 g, 24 mm diameter

## Slide 15: Kinetic Experiments

## Slide 16: Arrhenius Parameters
Microwave:
Ea=37.79(±1.96) kJ/mole
A=5.66x10-4 /sec
Thermal: Ea=113.43(±7.44) kJ/mol
A=4.86x10-1 /sec

## Slide 17: Product Composition
Gas Composition as a Function of Time and Temperature

## Slide 18
Equilibrium Determination

## Slide 19
Static Experiments
T(K) | T(K) Gas | Kp | ΔG( kJ/mol) | T(K) | Kp | ΔG (kJ/mol)
1086 | 267 | 68.3(±10.6) | -38.1(±1.3) | 1086 | 21.6 | -27.7
1185 | 380 | 85.2(­±9.1) | -43.8(±1.0) | 1185 | 117.43 | -47.0
1232 | 390 | 103(±6.66) | -47.5(±0.64) | 1232 | 238.7 | -56.1
1265 | 404 | 111(±0.17) | -49.6(±0.02) | 1265 | 380.7 | -62.5
Microwave
Thermal

## Slide 20
Enthalpy and Entropy
Van’t Hoff Plot
Microwave
ΔH = 33.4(±3.3) kJ/mole
ΔS =65.6 (±3.1) J/mol
Thermal
ΔH = 183.3 kJ/mole
ΔS = 194.3 J/mol

## Slide 21
Microwave Effect on the Equilibrium

## Slide 22
Gas-Carbon Equilibria
H2O + C D CO + H2 ΔH=+131 kJ/mol 1.
CO2 + C D 2CO ΔH=+172 kJ/mol 2.
CO + H2O D 2H2 + CO2 ΔH=-41 kJ/mol 3.
2H2 + C D CH4 ΔH=-75 kJ/mol 4.

## Slide 23
Graphite
Surface area: 7.6 m2/g
Loss tangent @ 2.45 GHz = 0.26(0.016)
Carbon Properties

## Slide 24
Equilibrium Composition

## Slide 25
T(K) | T(K) Gas | Kp | ΔG( kJ/mol) | T(K) | Kp | ΔG (kJ/mol)
764 | 293 | 3.19(±.53) | -7.4(±1.0) | 764 | 0.03 | 23.5
832 | 309 | 3.90(±.61) | -9.4(±1.0) | 832 | 0.16 | 12.8
893 | 321 | 4.39(±.43) | -11.0(±.7) | 893 | 0.66 | 3.12
949 | 331 | 4.95(±.50) | -12.6(±.8) | 949 | 2.07 | -5.74
997 | 337 | 5.61(±.48) | -14.3(±.7) | 997 | 4.99 | -13.33
Equilibrium and Free Energy for the Steam-Carbon Reaction
Microwave
Thermal

## Slide 26
 | Microwave |  | Thermal | 
 | ΔH (kJ/mol) | ΔS (J/K mol) | ΔH (kJ/mol) | ΔS (J/K mol)
Steam-C | 15.2 | 29.5 | 144.2 | 158.1
Boudouard | 27.0 | 43.1 | 180.2 | 191.2
Water-gas | -11.4 | -14.1 | -36.0 | -58.1
Carbon-H | -9.1 | -32.2 | -79.7 | -90.4
Thermodynamics of the Carbon-Steam Reaction in the Microwave

## Slide 27
Microwave Effect on the Equilibrium

## Slide 28
Thermodynamic Considerations of the Microwave Effect

## Slide 29
The microwave accelerates the forward reaction relative to the reverse reaction
Origin of Microwave Effect and a Proposed Mechanism

## Slide 30
Conclusion
Microwaves radiation can do far more than just heat a reaction or a catalyst.
It can change change both the apparent thermodynamics of the reactions and can affect the products of the reaction.

## Slide 31
Acknowledgements
Jake Hunt
Tony Ferrari
Mark Crosswhite
Adrian Lita
Bridgett Ashley
Tom Dusek
$$$ NSF and DOE

## Slide 32
Microwave Chemistry Working Group
FSU Chemistry
Al Stiegman
Greg Dudley
Geoff Strouse
Susan Latturner
FSU Chemical Engineering
John Telotte
Tyndall AFB
Jeff Owens
Bridgett Ashley
Derek Lovingood
chem.fsu.edu/mcwg